Mini enterprises

TOTAL POLYMER RELEASE

Mold Releaser (#135T): is a non-wax, non-silicone polymer

based Release agent fortified with high temp polymers for

high heat stability and accelerated exothermic heat releases

in newer composites. It provides Multiple Releases for all

Poly Ester Molds, Compression Molding, Vacuum Bagging

and Resin Transfer Molding - RTM.

APPLICATION WITH : FOAM /COTTONWOOL/TERRY TOWEL

PROCEDURE :APPLY FIVE COATS IN CIRCULAR CLOCKWISE MOTION,

COAT THE  EDGES AND CORNERS ONCE MORE CAREFULLY

DRYING TIME :15-20 MINUTES DEPENDING ON THE WEATHER

CONDITIONS BETWEEN EACH COAT

WIPE LIGHTLY WITH TERRY TOWEL TO GET EVENESS AND LITTLE SHINE

AFTER DRYING OF EACH COAT .

LEAVE THE MOLD FOR 15-20 MINS FOR THE FILM TO HARDEN.

RELEASE PARTS , WHEN THE PULL BECOMES HARD,APPLY ONE COAT AS

EXPLAINED EARLIER AND RELEASE PARTS TILL THE PULL GETS

HARDER.  REPEAT THE ABOVE ONE COAT STEP AGAIN

IF POROSITY SEALER IS USED THE NUMBER OF RELEASES WILL INCREASE.